QINGDAO RIWELL ADVANCED MATERIALS CO., LTD

Add: 1601, No. 230 Shenzhen Road, Qingdao 266101, China

Tel: +86 532 55576250  Fax: +86 532 55576210

Technical Data

| Item |  | PAN based graphite hard felt |
| --- | --- | --- |
| Density (g/cm3) |  | 0.16--0.20 |
| Thermal conductivity (W/m.k@1150℃) |  | 0.40 |
| Ash ( PPM) |  | 300 (max) |
| Carbon ( % ) |  | 99.00 (min) |
| Folding Strength ( Mpa) |  | 1.0 |
| Flexural Strength (Mpa) |  | 1.1 |
| Crushing stress at 5% compression (Mpa) |  | 0.6 |
| Processing Temperature °C |  | 2000 (min) |
| Operation Temperature °C | Atmosphere | 400 |
|  | Vacuum | 2000 |
|  | Inert gases | 3400 |
| Standard Size (mm) |  | 1500x1000x40 |